## Appendix 3.	Dendrochronological Results (Author: Nigel Nayling)

THE UNIVERSITY OF WALES LAMPETER ARCHAEOLOGICAL SERVICES

TREE-RING ANALYSIS OF SAMPLES FROM THE DESIGNATED HISTORIC WRECK SITE ‘THE DIAMOND’, CARDIGAN BAY

Dendrochronology Report 2006

October 2006

Report by

Nigel Nayling

| Prepared for: Ian Cundy Malvern Archaeological Diving Unit | Prepared by: Dendrochronology Laboratory, Dept of Archaeology and Anthropology, University of Wales Lampeter, Lampeter, Ceredigion, SA48 7ED |
| --- | --- |

TREE-RING ANALYSIS OF SAMPLES FROM THE DESIGNATED HISTORIC WRECK SITE ‘THE DIAMOND’, CARDIGAN BAY

## Introduction

This document is a technical archive report on the recovery and subsequent tree-ring analysis of samples taken from a wreck provisionally identified as the Diamond, located in Cardigan Bay and designated as an historic wreck under the provisions of the Protection of Wrecks Act 1973. This investigation and analysis were carried out under an excavation licence issued by Cadw: Welsh Historic Monuments, on behalf of the licensee, Ian Cundy of the Malvern Archaeological Diving Unit.

The aims of this study were to recover tree-ring samples for dating and possibly provenancing of timbers previously assessed as suitable for tree-ring dating (Nayling 2005).

Methodology

The site was dived on once by the author following limited excavation by Wessex Archaeology in 2004 (Nayling 2005). In addition to taking samples for species identification, exposed timbers were examined visually to assess their suitability for dendrochronological analysis. Most of the frames exposed in Trench 1 appeared to comprise quartered oak timbers with long tree ring sequences (c100 rings) making them potentially suitable for dendrochronological dating. The dendrochronological potential of the framing timbers was assessed as good. It was suggested that samples taken from multiple frames offered the potential to provide both dating and provenance for the timber used in the vessel’s construction. As a result, the licensee sought an excavation licence for the recovery of samples for tree-ring analysis.

In June 2006, the area in the vicinity of Trench 1 was re-excavated by members of the Malvern Archaeological Diving Unit and the author. A total of six samples were recovered over two days, using hand saws, from six different framing timbers assessed as suitable for tree-ring dating.

Prior to measurement, the samples were cleaned with razor blades to expose the fullest ring sequence. In the case of slice samples which comprised half or more of the complete cross-section of the parent tree, two radii were usually measured. The complete sequences of growth rings in the samples that were selected for dating purposes were measured to an accuracy of 0.01mm using a micro-computer based travelling stage. Cross-correlation algorithms (Baillie and Pilcher 1973; Munro 1984) were employed to search for positions where the ring sequences were highly correlated. The ring sequences were plotted electronically and exported to a computer graphics software package (Coreldraw™ v.8) to enable visual comparisons to be made between sequences at the positions indicated and, where these were satisfactory, new mean sequence was constructed from the synchronised sequences. The t-values reported below are derived from the original CROS algorithm (Baillie and Pilcher 1973). A t-value of 3.5 or over is usually indicative of a good match, although this is with the proviso that high t-values at the same relative or absolute position must be obtained from a range of independent sequences, and that satisfactory visual matching supports these positions.

All the measured sequences from this assemblage were compared with each other and those found to cross-match were combined to form a site master curve. The calculated site masters was tested against a range of reference chronologies from Britain, Europe and further afield to provide calendar dates for the ring-sequences, and identify a possible origin for the timber.

Results

A total of six samples were recovered for analysis. These are listed in Table 1 giving information on their nature and the results of analysis. Five of these samples cross-matched against each other exhibiting significant t-values between their ring-width series (Table 2), and close visual correspondence between their ring-width patterns. A 215-year ring width mean (NTD_T5) was calculated from the synchronised individual timber series and compared with oak ring-width means from Britain and Ireland without success. The mean was then compared with tree-ring chronologies available through the International Tree Ring Data Bank, and correlations found with tree-ring chronologies from the Great Lakes region of the Northern American continent (Table 3). These correlations indicate a date for the tree-ring mean of AD1614-AD1828 inclusive. The ring-width data for this mean are given in Table 4. The dating of individual timbers is indicated in Figure 1.

Figure 1 Bar diagram of dated tree-ring sequences from individual timbers (see Table 1 for details)

Comment

The sampling exercise proved very successful with the efforts of a small dive team using SCUBA resulting in the recovery of six viable samples. Analysis resulted in a well-replicated, long site mean. This does not appear to be British, and initial results suggest that the timber comes from the northern part of the North American continent. It is hoped that communications with dendrochronologists working in this area will help to confirm and refine these findings. It should be stressed that dendrochronological analysis can not determine whether or not the timber was traded for shipbuilding at a site some distance from the growing site, or which species of oak is represented. The dating indicates that the timber must have been felled some time after AD 1828. How much later can not be determined as no sapwood, bark edge or heartwood/sapwood boundary was found on any of the samples.

Acknowledgements

I am most grateful to Ian Cundy and members of the Malvern Archaeological Diving Unit for making the sampling exercise such a success and for advice and background information. This study has been funded through Cadw: Welsh Historic Monuments and its financial support is gratefully acknowledged.

Table 1 Sample details from 2006 fieldwork at the ‘Diamond’ designated historic wreck site

| Sample | Comments | Conversion | Dimensions | Total Rings | Average Ring Width (mm) | Date Range |
| --- | --- | --- | --- | --- | --- | --- |
| ntd01 | Slice sample from heavily bored framing timber | Quartered | 375 x 240 | 172 | 1.25 | AD 1614-AD 1785 |
| ntd02 | Slice sample from heavily bored framing timber | Quartered | 375 x 240 | 144 | 1.41 | AD 1683-AD 1826 |
| ntd03 | Wedge sample | Halved | 375 x 240 | 151 | 1.05 | undated |
| ntd04 | Wedge sample | Quartered | 375 x 240 | 210 | 1.24 | AD 1619-AD 1828 |
| ntd05 | Wedge sample | Quartered | 375 x 240 | 119 | 1.21 | AD 1703-AD 1821 |
| ntd06 | Wedge sample | Quartered | 375 x 240 | 185 | 1.30 | AD 1627-AD 1811 |

All samples were oak (Quercus spp.). No samples retained bark edge, sapwood or the heartwood sapwood boundary. No estimates of the felling date range of the individual timbers can be given therefore. As the origin of the timbers is not clear, a minimum number of sapwood rings cannot be applied.

Table 2    t-value matrix for cross-matched samples

| Sample | ntd02 | ntd04 | ntd05o | ntd06 |
| --- | --- | --- | --- | --- |
| ntd01 | 3.96 | 6.46 | 4.40 | 5.50 |
| ntd02 |  | 6.40 | 4.52 | 6.44 |
| ntd04 |  |  | 5.08 | 7.96 |
| ntd05 |  |  |  | 5.71 |

Table 3    Correlations between the five timber, 215-year mean NYT_T5, and chronologies from the Great Lakes region of northern America. t-value matrix for cross-matched samples

| ITRDB Chronology Code | Description | Date Start | Date End | t-value |
| --- | --- | --- | --- | --- |
| WI004 | Bass Lake Peninsula - Standard Wisconsin, Mid USA (Ed Cook) | AD 1595 | AD 1983 | 5.21 |
| MI005 | Cranbrook Institute - Standard Michigan, Mid USA (Ed Cook) | AD 1581 | AD 1983 | 5.67 |
| OH002 | Stebbin's Gulch; Holden Arb. Standard Ohio, NE USA (Ed Cook) | AD 1612 | AD 1983 | 5.73 |

Table 4    Tree-ring widths for the five timber, 215-year mean NYT_T5, dated to AD 1614-AD 1828 inclusive

| Date | Mean Ring Width (mm) | Number of Timber |
| --- | --- | --- |
| AD 1614 |  |  |  | 145 | 131 | 109 | 127 | 146 | 168 | 147 |  |  |  | 1 | 1 | 1 | 1 | 1 | 2 | 2 |
| - | 158 | 140 | 128 | 150 | 127 | 140 | 125 | 152 | 111 | 126 | 2 | 2 | 2 | 2 | 2 | 2 | 3 | 3 | 3 | 3 |
| - | 148 | 120 | 108 | 101 | 84 | 139 | 164 | 198 | 189 | 188 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 |
| - | 143 | 150 | 175 | 167 | 126 | 132 | 178 | 140 | 136 | 87 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 |
| AD 1651 | 131 | 174 | 178 | 130 | 131 | 181 | 146 | 144 | 161 | 157 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 |
| - | 169 | 161 | 154 | 89 | 91 | 136 | 158 | 202 | 175 | 146 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 |
| - | 157 | 152 | 147 | 144 | 150 | 126 | 113 | 128 | 120 | 128 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 |
| - | 99 | 110 | 135 | 148 | 128 | 177 | 171 | 169 | 162 | 154 | 3 | 3 | 4 | 4 | 4 | 4 | 4 | 4 | 4 | 4 |
| - | 135 | 154 | 150 | 110 | 147 | 147 | 125 | 115 | 140 | 120 | 4 | 4 | 4 | 4 | 4 | 4 | 4 | 4 | 4 | 4 |
| AD 1701 | 137 | 139 | 151 | 118 | 119 | 134 | 144 | 139 | 104 | 131 | 4 | 4 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 |
| - | 113 | 133 | 128 | 142 | 141 | 133 | 133 | 128 | 141 | 85 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 |
| - | 99 | 118 | 104 | 119 | 135 | 114 | 140 | 151 | 159 | 181 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 |
| - | 136 | 132 | 112 | 114 | 112 | 120 | 140 | 105 | 92 | 95 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 |
| - | 93 | 69 | 75 | 102 | 116 | 115 | 117 | 94 | 114 | 148 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 |
| AD 1751 | 151 | 133 | 129 | 154 | 139 | 191 | 106 | 139 | 155 | 129 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 |
| - | 110 | 123 | 120 | 130 | 121 | 154 | 124 | 139 | 103 | 110 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 |
| - | 90 | 122 | 128 | 129 | 134 | 148 | 139 | 131 | 129 | 126 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 |
| - | 107 | 118 | 111 | 115 | 111 | 132 | 160 | 111 | 92 | 111 | 5 | 5 | 5 | 5 | 5 | 4 | 4 | 4 | 4 | 4 |
| - | 93 | 112 | 111 | 108 | 105 | 100 | 118 | 104 | 96 | 98 | 4 | 4 | 4 | 4 | 4 | 4 | 4 | 4 | 4 | 4 |
| AD 1801 | 124 | 91 | 84 | 112 | 111 | 89 | 99 | 117 | 95 | 116 | 4 | 4 | 4 | 4 | 4 | 4 | 4 | 4 | 4 | 4 |
| - | 111 | 122 | 116 | 114 | 109 | 121 | 151 | 115 | 117 | 86 | 4 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 |
| - | 100 | 119 | 105 | 127 | 100 | 114 | 169 | 135 |  |  | 3 | 2 | 2 | 2 | 2 | 2 | 1 | 1 |  |  |

References

Baillie, M G L, and Pilcher, J R, 1973 A simple crossdating program for tree-ring research, Tree Ring Bulletin, 33, 7-14

English Heritage, 1998 Dendrochronology: guidelines on producing and interpreting dendrochronological dates, London

Munro, M A R, 1984 An improved algorithm for crossdating tree-ring series, Tree Ring Bulletin, 44, 17-27

Nayling, N, 2005 Wood Identification of Samples from the Designated Historic Wreck Site ‘The Diamond’, Cardigan Bay. UWLAS Dendrochronology Report 2005/01